Physicochemical characterization and antibacterial activity of alginate-encapsulated essential oils of Origanum vulgare L. and Thymus vulgaris L. against canine and feline uropathogens

Camilla Torres Pereira1

ORCID: https://orcid.org/0000-0002-5686-1841

E-mail: camilla.torres.cb@gmail.com

Bernadete Santos1

ORCID: https://orcid.org/0000-0003-4234-4752

E-mail: bernadetes672@gmail.com

Mylena Medeiros Simões1

ORCID: https://orcid.org/0000-0002-0654-4733

E-mail:mylenamedeirossimoes@gmail.com

Millena de Souza Alves1

ORCID: https://orcid.org/0000-0002-7981-7608

E-mail: millenaasouzaa@gmail.com

Fernanda Matias Cariri Marques1

ORCID: https://orcid.org/0000-0001-5571-1596

E-mail: fernandacariri20@gmail.com

Maria Alice Araújo de Medeiros1

ORCID: https://orcid.org/0000-0001-5563-7955

E-mail: medeirosallice22@gmail.com

João Henrique Anizio de Farias1

ORCID: https://orcid.org/0000-0003-0843-2142

E-mail: henriqueanizio7@gmail.com

Wladymyr Jefferson Bacalhau de Sousa2

ORCID: https://orcid.org/0000-0002-3931-8265

E-mail: Wladymyrjb@gmail.com

Albaniza Alves Tavares2

ORCID: https://orcid.org/0000-0003-1412-4787

E-mail: albaniza.alves@gmail.com

Abrahão Alves de Oliveira Filho3

ORCID: https://orcid.org/0000-0002-7466-9933

E-mail: abrahao.farm@gmail.com

Affiliations

1 Federal University of Campina Grande (UFCG), Graduate Program in Animal Science and Health, Patos, PB, Brazil.

2 Federal University of Campina Grande (UFCG), Postgraduate Program in Materials Science and Engineering, Campina Grande, PB, Brazil.

3 Federal University of Campina Grande (UFCG), Patos, PB, Brazil

.

Abstract

Urinary tract infections are common in small animal practice, with Escherichia coli and Klebsiella pneumoniae being the primary causative agents. Bacterial resistance to synthetic antimicrobials has driven the search for natural alternatives, such as essential oils, whose direct application is limited by their volatility and instability. The objective of this study was to characterize, both physicochemically and morphologically, alginate capsules containing a mixture of essential oils from Origanum vulgare L. and Thymus vulgaris L., as well as to evaluate, in a complementary manner, their antibacterial activity against uropathogenic bacteria isolated from dogs and cats. The capsules were obtained by ionic gelation and characterized in terms of physical properties, water activity, moisture content, and morphology. Antibacterial activity was evaluated using the agar diffusion method. The encapsulated systems exhibited parameters consistent with good flowability, physicochemical stability, and a water activity below 0.7. Furthermore, the capsules containing the essential oils maintained antibacterial activity, evidenced by the formation of inhibition zones against the evaluated strains. It is concluded that alginate encapsulation constitutes a promising strategy for the protection and application of essential oils with potential use in the control of uropathogenic pathogens in veterinary medicine.

Keywords: Alginate capsules; Carvacrol; Thymol; Uropathogenic bacteria; Companion animals.

1. INTRODUCTION

Urinary tract infections (UTIs) are among the most common bacterial diseases diagnosed in small animal practice, particularly in dogs and cats, with Escherichia coli and Klebsiella pneumoniae being the primary causative agents associated with these conditions (Sousa et al., 2019; Silva et al., 2025). Treatment of these infections is often based on the use of synthetic antibiotics, frequently administered empirically and repeatedly, which favors the selection of multidrug-resistant strains in the veterinary setting (Sellera et al., 2025). This scenario has been widely described in urinary isolates from small animals and is associated with treatment failures, recurrence of infections, and increased costs related to clinical management (Scarpellini et al., 2025).

In this context, essential oils have attracted growing interest as natural alternatives due to their antibacterial activity and their efficacy against different groups of bacteria (Matte et al., 2023). These plant-derived compounds have the potential to inhibit the growth and reproduction of pathogenic microorganisms. Furthermore, their use does not tend to promote the development of microbial resistance, as they possess a complex structure and thus attack multiple targets within the cells of microorganisms, making them effective in controlling clinically relevant pathogens (Nuță et al., 2021; Cui et al., 2024).

The essential oils of Origanum vulgare and Thymus vulgaris have been studied for their activity against bacterial pathogens, including Gram-negative species, which is attributed primarily to the presence of phenolic compounds such as thymol and carvacrol (Cui et al., 2024). These constituents act by disrupting the bacterial cell membrane, resulting in the inhibition of growth or death of the microorganisms.

Despite their recognized antibacterial potential, the direct application of essential oils has limitations, such as high volatility and instability in the face of environmental factors, which can compromise their efficacy (Nuță et al., 2021), especially in complex biological systems such as the urinary tract. Consequently, encapsulation has been employed as a strategy to protect bioactive compounds, increase stability, and promote controlled release, thereby expanding the application possibilities of these systems (Nuță et al., 2021; Štrbac et al., 2021).

The objective of this study was to characterize the physicochemical and morphological properties of the encapsulation systems employed, as well as to evaluate capsules containing a mixture of essential oils from Origanum vulgare L. and Thymus vulgaris L. for their antibacterial activity against strains isolated from urinary tract infections in dogs and cats.

2. MATERIALS AND METHODS

This study was approved by the Animal Ethics Committee of the Federal University of Campina Grande (CEUA/CSTR/UFCG), protocol number 022026.

2.1 Location of the Experimental Tests and Test Substances

The experimental tests were conducted at the Microbiology and Biochemistry Laboratories of the Central Laboratories of the Academic Unit of Biological Sciences (UACB) at the Federal University of Campina Grande (UFCG), Patos Campus, Paraíba, Brazil. The essential oils of Origanum vulgare L. (oregano) and Thymus vulgaris L. (thyme) were purchased from a certified commercial supplier (Quinarí®, Ponta Grossa, Paraná, Brazil). The samples were stored in amber vials, refrigerated (4 °C), and protected from light until use.

2.2 Bacterial Strains and Culture Media

Clinical strains of Escherichia coli isolated from dogs (Ecc 49) and cats (Ecg 13) were used, as well as strains of Klebsiella pneumoniae (Kp 04) isolated from dogs, obtained from urine samples of animals with a clinical diagnosis of urinary tract infection. The bacterial strains were maintained on Mueller-Hinton agar (MHA) at 4 °C until the tests were performed. Inocula were prepared from fresh cultures on MHA incubated at 35 ± 2 °C for 18–24 h, and subsequently diluted in 0.9% sterile saline until a turbidity equivalent to 0.5 on the McFarland scale was obtained, corresponding to approximately 1.5 × 10⁸ colony-forming units per milliliter (CFU/mL) (Bona et al., 2014).

2.3 Analysis by Gas Chromatography Coupled with Mass Spectrometry (GC-MS)

The chemical composition of the essential oil was analyzed using a gas chromatograph coupled with a quadrupole mass spectrometer (GC-MS), Shimadzu, model GC-QP2010 (Shimadzu, Kyoto, Japan). A DB-5 fused silica capillary column (30 m × 0.25 mm i.d. × 0.25 μm) was used.

The chromatographic conditions employed were: injector temperature of 220 °C, split ratio of 1:10 (3.0 min), helium (He) carrier gas at a flow rate of 0.6 mL/min, interface temperature of 250 °C, and an electron impact ionization source operating in the 35–350 m/z range. The oven temperature ramp was programmed to start at 40 °C (held for 2 min), followed by an increase of 3 °C/min to 240 °C, remaining at that temperature for 5 min. The injection volume was 1 μL of a 1% solution in dichloromethane.

Compound identification was performed by comparing fragmentation patterns with mass spectra from the NIST 14 database (Mass Spectral Library, 2014), available on the CG-EM system. Additionally, the compounds were identified by comparison with data from the literature (Adams, 2007) and using linear retention indices (LRI), calculated based on the retention times of a homologous series of hydrocarbons (C8 to C26), injected under the same chromatographic conditions as the sample. The linear retention index was calculated using the methods described by Van den Dool and Kratz (1963) and Adams (2007). For identification by comparison with spectra available in databases, only matches exceeding 90% were considered.

2.4 Encapsulation of oregano and thyme essential oils in alginate

2.4.1 Formulations and concentrations

The encapsulation of the essential oils of Origanum vulgare L. (oregano) and Thymus vulgaris L. (thyme) was performed according to the methodology described by Pagani et al. (2014), with modifications. Initially, a 2% (w/v) sodium alginate solution and a 2% (w/v) calcium chloride solution were prepared, both using distilled water that had been previously heat-treated to remove potential contaminants.

The sodium alginate-based capsules were prepared by individually incorporating essential oils into the polymer solution at a concentration of 20% (v/v). After complete homogenization, the mixture was dispensed, using an automatic pipette, into the calcium chloride solution, resulting in the formation of the capsules through the ionic gelation process.

2.4.2 Gelation and Drying Process

The capsules remained in the calcium chloride solution for 60 seconds, after which they were collected and washed with distilled water to remove excess calcium ions. The capsules were then dried in a forced-air oven at 50 ± 2 °C for 32 hours. After drying, the capsules were packaged in sterile containers and stored under appropriate conditions until use (Ferreira et al., 2021).

2.5 Physicochemical and morphological characterization of capsules containing oregano and thyme essential oils

2.5.1 Measurement of capsule diameter and sphericity factor (SF)

The diameter of the capsules was determined by measuring a sample of 30 capsules from each formulation using a digital caliper with an accuracy of 0.01 mm (Mitutoyo®). For each capsule, the major diameter (dM) and minor diameter (dm) were measured, as described by Asha et al. (2011).

The sphericity factor of the capsules was calculated from the values of the major and minor diameters using the following equation: SF = (dM – dm) / (dM + dm)

2.5.2 Density, Compressibility Index, and Hausner Factor

The compressibility index (CI) was determined from the values of bulk density (BD) and compacted density (CD), according to the equation proposed by Carr (1965) and adopted by official compendia such as the United States Pharmacopeia (USP): CI = (CD – BD) / CD × 100.

The Hausner factor (HF) was determined by the ratio of compacted density (CD) to bulk density (BD), as described by Hausner (1967) and in accordance with the recommendations of the United States Pharmacopeia (USP, 2022), and was used as an indicator of the material’s flow and compressibility properties.

2.5.3 Water activity (Aw) and moisture content of the capsules

The water activity (Aw) of the capsules was determined using the AquaLab® (Dew Point Water Activity Meter 4TEV) instrument, in accordance with the official methodology (NOM, 2008). Aw represents the ratio between the vapor pressure of the water present in the sample and the vapor pressure of pure water at the same temperature (Badui, 2006).

Moisture content was determined according to AOAC (1997), method 925.01, by keeping the samples in an oven at 105 °C until constant weight was reached. The moisture percentage was calculated using the equation: %U = (m_(a,i) – m_(a,f)) / m_(a,i) × 100

where: %U = moisture percentage; m_(a,i) = initial mass of the sample; m_(a,f) = final mass of the sample.

2.5.4 Scanning electron microscopy (SEM)

Morphological analysis of the samples was performed using scanning electron microscopy (SEM), in accordance with the procedures described by Rosenberg and Young (1993). In this analysis, the samples were first dehydrated in 70%, 90%, and 100% alcohol, using 1 mL per sample and a contact time of 10 minutes for each of the alcohols applied, and  then the samples were dried in a dryer (Quorum/K 850) at the critical point with anhydrous CO₂ (1100 psi/31°C). The samples were then mounted on the analysis plate using colloidal silver and transferred to a metallizer (Quorum/Q 150R ES) to receive a thin layer of a metal alloy composed of gold and palladium. After metallization, the samples were examined using a scanning electron microscope (Philips – XL30 ESEM) operating at 10 kV.

2.5.5 Infrared Spectroscopy Analysis (FTIR/IR)

The spectra of the samples were analyzed using a mid-infrared FTIR-ATR instrument (Cary 630 FTIR, Agilent Technologies Inc., Santa Clara, CA, USA), equipped with an attenuated total reflectance (ATR) cell, in accordance with the manufacturer’s specifications (Agilent Technologies Inc., 2015). The analyses were performed in the spectral region ranging from 4000 cm⁻¹ to 600 cm⁻¹, with the spectra obtained in absorption mode, a methodology widely used for the characterization of materials by infrared spectroscopy (Smith, 2018).

During the analysis, the ambient temperature was maintained at 25 °C, and prior to each measurement, the background spectrum was recorded, a procedure necessary for correcting instrumental interferences. Next, 0.5 g of the sample was placed on the surface of the diamond crystal, where infrared rays strike to perform the attenuated total reflectance spectral measurement (Smith, 2018). Spectral data were acquired using Microlab PC software, provided by the equipment manufacturer (Agilent Technologies Inc., 2015).

2.6 Antibacterial activity of oregano and thyme essential oil capsules

The testing technique was developed according to Bona et al. (2014), with modifications. For this purpose, the strains were inoculated onto Petri dishes containing Mueller-Hinton agar, and using a template, 6-mm-diameter holes were made in the center to create the wells. The capsules containing the essential oils of Origanum vulgare L. and Thymus vulgaris L. were aseptically deposited into the wells, and the plates were then incubated in a bacterial incubator at 35 ± 2 °C for 24 hours. After incubation, the plates were examined for uniform bacterial growth, and in cases where growth inhibition was observed, the diameter of the zone of inhibition was measured using a millimeter ruler. The tests were performed in duplicate, and the results represent the mean values.

3. RESULTS

Analysis of the total ion chromatograms obtained by GC-MS, shown in Table 1, allowed for the identification of the main chemical constituents of the essential oils evaluated. A predominance of phenolic monoterpenes was observed, notably thymol in thyme essential oil (67.5%) and carvacrol in oregano essential oil (83.8%).

[Table 1]

The physicochemical characterization of the capsules containing the essential oils of Origanum vulgare and Thymus vulgaris, presented in Table 2, revealed parameters consistent with stable encapsulated systems suitable for biological applications.

[Table 2]

Scanning electron microscopy analysis in Figure 1 revealed that the alginate spheres containing oregano and thyme essential oils have a rough, irregular, and heterogeneous surface.

[Figure 1]

The FTIR-ATR spectra of pure sodium alginate and the alginate capsules containing oregano and thyme essential oils, prepared from the stock solution, showed similar profiles, with no significant changes in the characteristic bands of the polymeric matrix, such as those attributed to the –COO⁻, –C–O–C, and –OH groups.

Regarding antibacterial activity, the combination of Origanum vulgare and Thymus vulgaris essential oils at a 20% concentration was able to inhibit the growth of the evaluated bacterial strains, as evidenced by the formation of inhibition zones ranging from 12 to 16 mm, as shown in Table 3.

[Table 3]

4. DISCUSSION

Compounds such as thymol and carvacrol are widely recognized for their antimicrobial properties, which reinforces the biological potential of the essential oils studied (Cui et al., 2024). Furthermore, the identification of the major constituents is essential for establishing reference parameters, enabling the evaluation of the encapsulation process’s efficiency in subsequent stages.

Regarding the physicochemical characterization of the capsules, the values for bulk and tapped density showed little variation among themselves, directly reflecting the low compressibility index and a Hausner factor close to unity. These results indicate good flowability and low cohesiveness of the material, characteristics that are fundamental for the processing, storage, and standardization of encapsulated systems (Carr, 1965; Hausner, 1967).

The average diameter of the capsules, combined with the sphericity factor, suggests the formation of relatively homogeneous particles, although not perfectly spherical. This morphology is observed in encapsulated systems obtained by droplet formation and ionic gelation, such as alginate capsules, and is related to the characteristics of the particle formation process (Martins et al., 2017). Uniformity in dimensions and a shape close to a sphere favor greater controlled release of bioactive compounds, in addition to contributing to the physical stability of the encapsulated system (Karim et al., 2022).

The observed moisture and water activity values indicate conditions favorable to the physicochemical and microbiological stability of the capsules. A water activity below 0.7 indicates low availability of free water in the system, a parameter directly related to the reduction of the risk of microbial growth and the slowing of chemical degradation reactions (Labuza, 1980; Guadarrama-Lezama et al., 2014). This aspect is particularly relevant in encapsulated systems containing essential oils, since low water activity contributes to the protection of volatile and phenolic compounds, reducing oxidation processes and losses due to volatilization during storage (Guadarrama-Lezama et al., 2014). Furthermore, recent studies have shown that alginate-based polymer systems exhibit greater structural stability and better preservation of the biological activity of the encapsulated compounds when maintained within narrow ranges of water activity, reinforcing the validity of the values obtained in the present study (Dodero et al. 2021).

The rough, irregular, and heterogeneous surface of the analyzed capsule indicates that this morphology is primarily associated with the differential contraction of the polymer matrix during the gelation and drying processes, which promote intense water removal and consequent structural shrinkage, resulting in the formation of surface roughness and microcracks (Vargas et al., 2018).

The results, showing no significant changes in the characteristic bands of the polymer matrix, indicate that the incorporation of essential oils did not promote structural modifications detectable by this technique, suggesting that the interaction between the bioactive compounds and sodium alginate occurred predominantly in a physical manner, without the formation of new chemical bonds.

The absence of bands attributed to the major constituents of essential oils, such as carvacrol and thymol, may be associated with the incorporation of these compounds into the sodium alginate polymer matrix, as well as with their low concentration in the system. Due to their hydrophobic nature, essential oil compounds tend to disperse as droplets within the matrix, potentially interacting with the polymer and becoming difficult to identify by FTIR. Similar results have been reported in the literature for active polymeric films and materials containing extracts or essential oils, in which the incorporation of bioactive compounds did not result in significant changes in FTIR spectra, especially at low concentrations (Atarés; Chiralt, 2016; Johnson et al., 2023).

Encapsulated essential oils may retain the ability to inhibit microbial growth, evidenced by the formation of inhibition halos, when compared to free-form oils (Bona et al., 2014; Mostaghimi et al., 2023). Furthermore, the reduction in alginate and CaCl₂ concentrations resulted in greater release of essential oils due to the formation of a less compact polymeric network with a lower degree of ionic cross-linking. This more porous structure facilitates the diffusion of the encapsulated compounds, promoting faster and more intense release of the essential oils into the culture medium (Mostaghimi et al., 2023).

The variation in the diameters of the halos observed among the strains may be related to intrinsic differences in bacterial susceptibility, as well as to the composition and concentration of the phenolic compounds present in the essential oils, particularly thymol and carvacrol (Cui et al., 2024). These compounds are described in the literature as capable of acting in a complementary manner, promoting cell membrane disruption, increased permeability, and leakage of intracellular constituents, which may result in an additive antimicrobial effect when used in combination (Hamza et al., 2023).

The correlation between the physicochemical parameters of the capsules and the antibacterial activity observed against uropathogenic strains indicates that the encapsulation process acts primarily as a strategy for protecting and modulating the release of essential oils, rather than as a mechanism for directly increasing antibacterial potency. Encapsulation in an alginate matrix may contribute to the preservation of bioactive compounds, reducing losses due to volatilization, oxidation, and degradation during storage and application (Bakry et al., 2016; Dodero et al., 2021).

In addition, encapsulated systems have the potential to promote the gradual release of active ingredients, helping to maintain effective concentrations over time and increasing the viability of using these compounds as natural alternatives for controlling uropathogenic pathogens isolated from dogs and cats, especially in light of the growing problem of antibiotic resistance (Štrbac et al., 2021).

5. CONCLUSION

The physicochemical characterization of the capsules revealed properties consistent with stable encapsulated systems, including good flowability, homogeneous morphology, and low water activity values, indicating conditions favorable to physicochemical and microbiological stability and reinforcing the role of encapsulation in protecting and maintaining the biological activity of essential oils. The combination of essential oils from Origanum vulgare L. and Thymus vulgaris L., encapsulated in an alginate matrix, exhibited antibacterial activity against uropathogenic strains of Escherichia coli and Klebsiella pneumoniae isolated from dogs and cats, as evidenced by in vitro inhibition zones. Thus, the encapsulated systems show potential as a natural alternative for controlling uropathogenic pathogens of veterinary importance, given the growing scenario of antimicrobial resistance in small animals, highlighting the need for future studies to optimize formulations and evaluate them in more complex biological models.

FUNDING

This study was funded by the Coordination for the Improvement of Higher Education Personnel (CAPES) – Brazil.

CONFLICT OF INTEREST

The authors declare no conflict of interest.

DATA AVAILABILITY

All data are available in the article.

ETHICS STATEMENT

This research was reviewed and approved by the Animal Ethics Committee of the Federal University of Campina Grande (CEUA/CSTR/UFCG), under protocol number 022026.

AUTHORS’ CONTRIBUTIONS

CTP conducted the essential oil encapsulation experiments, performed the physicochemical and morphological characterization of the capsules, conducted the antibacterial activity assays, analyzed and interpreted the data, and drafted the manuscript. BS and MMS assisted in sample preparation, capsule processing, and laboratory analyses. JHAF contributed to the microbiological procedures and the collection of experimental data. MSA and FMCM contributed to the interpretation of the microbiological results and reviewed the methodology applied. WFBS and AAT performed sample preparation, image acquisition, and morphological analysis by scanning electron microscopy (SEM). MAAM participated in the discussion of the data and the critical review of the manuscript. AAOF supervised the study, contributed to the experimental design, and critically reviewed the final version of the manuscript. All authors read and approved the final version of the manuscript.

STATEMENT ON GENERATIVE AI

The authors declare that no generative AI was used in the writing of this manuscript.

REFERENCES

Adams, R.P. 2007. Identification of essential oil components by gas chromatography/mass spectrometry. 4th ed. Carol Stream: Allured Publishing Corporation.

Agilent Technologies Inc. 2015. Cary 630 FTIR spectrometer: user guide. Santa Clara, CA: Agilent Technologies.

Asha, P., Ramesh, K., Srinivasan, S. 2011. Preparation and characterization of alginate beads for controlled release applications. Journal of Applied Polymer Science, 119: 321–329. https://doi.org/10.1002/app.33821

Association of Official Analytical Chemists (AOAC). 1997. Official methods of analysis. Arlington, VA, USA: AOAC.

Atarés, L., Chiralt, A. 2016. Essential oils as additives in biodegradable films. Trends in Food Science & Technology, 48: 51–62. https://doi.org/10.1016/j.tifs.2015.12.001

Badui, D.S. 2006. Química de los alimentos. 4th ed. México: Pearson Educación.

Bakry, A.M., Abbas, S., Ali, B., Majeed, H., Abouelwafa, M.Y., Mousa, A., Liang, L. 2016. Microencapsulation of oils: a comprehensive review of benefits, techniques, and applications. Comprehensive Reviews in Food Science and Food Safety, 15(1): 143–182. https://doi.org/10.1111/1541-4337.12179

Bona, E.A.M., Pinto, F.G.S., Fruet, T.K., Jorge, T.C.M., Moura, A.C. 2014. Comparação de métodos para avaliação da atividade antimicrobiana e determinação da concentração inibitória mínima (CIM) de extratos vegetais aquosos e etanólicos. Arquivos do Instituto Biológico, 81(3): 218–225. https://doi.org/10.1590/1808-1657001192012

Carr, R.L. 1965. Evaluating flow properties of solids. Chemical Engineering,72:163–168.

Cui, H., Zhang, C., Li, C., Lin, L. 2024. Oregano essential oil in livestock and veterinary medicine. Animals, 14(11): 1532. https://doi.org/10.3390/ani14111532

Dodero, A., Alloisio, M., Vicini, S., Castellano, M. 2021. An up-to-date review on alginate nanoparticles and nanofibers for biomedical and pharmaceutical applications. Advanced Materials Interfaces, 8(22): 2100809. https://doi.org/10.1002/admi.202100809

Ferreira, L.P.C., Xavier, A.C.R., Santos, J., Wartha, E.R.S.A., Pagani, A.A.C. 2021. Microencapsulation of beet (Beta vulgaris L.) by ionic gelation process. Research, Society and Development, 10(12): e454101220171. https://doi.org/10.33448/rsd-v10i12.20171

Guadarrama, A.Y.L., Rodríguez-Huezo, M.E., Lobato-Calleros, C., Vernon-Carter, E.J., Alvarez-Ramírez, J. 2014. Effects of storage temperature and water activity on the degradation of carotenoids contained in microencapsulated chili extract. Drying Technology, 32(12): 1435–1447. https://doi.org/10.1080/07373937.2014.900502

Hamza, A.A., Al-Hassani, M.K. 2023. Biofilm formation and antimicrobial resistance in Serratia marcescens isolated from different clinical cases. Journal of Population Therapeutics and Clinical Pharmacology, 30(7): 460–465. https://doi.org/10.47750/jptcp.2023.30.07.051

Hausner, H.H. 1967. Friction conditions in a mass of metal powder. International Journal of Powder Metallurgy, 3(4): 7–13.

Johnson, J.B., Walsh, K.B., Naiker, M., Ameer, K. 2023. The use of infrared spectroscopy for quantification of bioactive compounds. Molecules, 28(7): 3215. https://doi.org/10.3390/molecules28073215

Karim, A., Alzubaidi, A., Haque, M.A., Islam, M.T., Uddin, M.N. 2022. Alginate-based nanocarriers for the delivery and controlled-release of bioactive compounds. Advances in Colloid and Interface Science, 307: 102744. https://doi.org/10.1016/j.cis.2022.102744

Labuza, T.P. 1980. The effect of water activity on reaction kinetics of food deterioration. Food Technology, 34: 36–41.

Martins, E., Poncelet, D., Rodrigues, R.C., Renard, D. 2017. Oil encapsulation techniques using alginate as encapsulating agent: applications and drawbacks. Journal of Microencapsulation, 34(8): 754–771. https://doi.org/10.1080/02652048.2017.1403495

Matte, E.H.C., Luciano, F.B., Evangelista, A.G. 2023. Essential oils and essential oil compounds in animal production as antimicrobials and anthelmintics: an updated review. Animal Health Research Reviews, 24(1): 1–11. https://doi.org/10.1017/S1466252322000093

Mostaghimi, M., Ghasemzadeh-Mohammadi, V., Akbari-Alavijeh, S., Hosseini, S.M. 2023. Development and characterization of antimicrobial alginate hydrogel beads filled with cinnamon essential oil nanoemulsion. Journal of Biomaterials Science, Polymer Edition, 34(15): 2144–2160. https://doi.org/10.1080/09205063.2023.2230843

Norma Oficial Mexicana NOM-247-SSA1-2008. 2008. Productos y servicios. México: Secretaría de Salud.

Nuță, D.C., Missir, A.V., Popa, G.L., Costea, T., Chirita, C. 2021. Contribution of essential oils to the fight against microbial biofilms—a review. Processes, 9(3): 537. https://doi.org/10.3390/pr9030537

Pagani, A.A.C., Oliveira, M.C., Xavier, A.C.R., Morais, A.L.B., Nunes, T.P., Silva, G.F. 2014. Study of the process of getting the drops of papaya (Carica papaya) per basic spherification. International Journal of Engineering and Innovative Technology, 4(6): 1-9.

Rosenberg, M., Young, S.L. 1993. Water activity: theory and application to food. New York: Academic Press.

Scarpellini, R., Stefanetti, V., Cappelli, K., Capomaccio, S., Passamonti, F. 2025. Antimicrobial resistance in companion animals. Animals, 15(11): 1547. https://doi.org/10.3390/ani15111547

Sellera, F.P., Silva, L.C., Moura, Q., Fuga, B., Fontana, H., Esposito, F., Lincopan, N. 2025. Strengthening clinical alliances to tackle antimicrobial resistance. Diagnostic Microbiology and Infectious Disease. https://doi.org/10.1016/j.diagmicrobio.2025.117231

Silva, J.M., Menezes, J., Fernandes, L., Marques, C., Santos Costa, S., Timofte, D., Amaral, A.J., Pomba, C. 2025. Evaluation of multidrug-resistant bacteria in veterinary practices. Frontiers in Cellular and Infection Microbiology, 15: 1582411. https://doi.org/10.3389/fcimb.2025.1582411

Smith, B.C. 2018. Infrared spectral interpretation: a systematic approach. 2nd ed. Boca Raton: CRC Press.

Sousa, A.T.H.I., Makino, H., Bruno, V.C.M., Candido, S.L., Nogueira, B.S., Menezes, I.G., Dutra, V. 2019. Perfil de resistência antimicrobiana de Klebsiella pneumoniae. Arquivo Brasileiro de Medicina Veterinária e Zootecnia, 71(2): 584–593. https://doi.org/10.1590/1678-4162-10599

Štrbac, F., Petrović, K., Stojanović, D., Ratajac, R. 2021. Possibilities and limitations of essential oils in dogs and cats. Veterinary Journal of Republic of Srpska, 21(1–2): 238–251.

United States Pharmacopeia (USP). 2022. <616> Bulk density and tapped density of powders. Rockville: USP Convention.

Van den Dool, H.A.N.D., Kratz, P.D. 1963. A generalization of the retention index system. Journal of Chromatography, 11: 463–471.

Vargas, P.O., Pereira, N.R., Guimaraes, A.O., Waldman, W.R., Pereira, V.R. 2018. Shrinkage and deformation during convective drying of calcium alginate. LWT – Food Science and Technology, 97: 213–222. https://doi.org/10.1016/j.lwt.2018.06.056

Table 1. Chemical constituents of oregano and thyme essential oils obtained by GC-MS.

| Essential oil | Compound | TR (min) | Area (%) |
| --- | --- | --- | --- |
| Oregano | p-cymene | 12,22 | 7,1 |
| Oregano | γ-terpinene | 13,82 | 3,0 |
| Oregano | Carvacrol | 25,8 | 83,8 |
| Oregano | Caryophyllene | 30,53 | 6,0 |
| Thyme | p-Cymene | 12,4 | 24,0 |
| Thyme | Linalool | 16,0 | 3,9 |
| Thyme | Thymol | 25,4 | 67,5 |
| Thyme | 2-Ethyl-4,5-dimethylphenol | 25,6 | 4,5 |

Table 2.  Physicochemical properties of capsules containing a mixture of essential oils.

| Parameter | Measured Value |
| --- | --- |
| Bulk density (BD) | 0,80 g/mL |
| Tapped density (TD) | 0,83 g/mL |
| Average diameter | 1,27 mm |
| Sphericity factor (SF) | 0,24 |
| Compressibility index (Carr) | 3,61 % |
| Hausner factor | 1,04 |
| Moisture content | 17,58 % |
| Water activity (aw) | 0,66 |

Figure 1 – Scanning electron microscope (SEM) images at 1000× magnification of the alginate sphere containing oregano and thyme.

Table 3. Inhibition zones (mm) obtained by the combination of oregano and thyme essential oils encapsulated at a concentration of 20% against the tested bacterial strains.

| Bacterial strain | Animal species | Identification | Inhibition zone (mm) |
| --- | --- | --- | --- |
| Escherichia coli | Cat | ECG 13 | 14 |
| Escherichia coli | Dog | ECC 49 | 16 |
| Klebsiella pneumoniae | Dog | KP 04 | 12 |