Evaluation of Simulated Ultrasonic Wash and UVC Light Fastness of Natural Textiles Dyed with Radermachera ignea Extracts

Khatha Wathakit

The Center for Plant Genetic Conservation Project Under the Royal Initiative of Her Royal Highness Princess Maha Chakri Sirindhorn of Suranaree University of Technology, Nakhon Ratchasima, Thailand

E-mail: vkata@sut.ac.th

ORCID id: https://orcid.org/0000-0002-0138-032X

Sakaya Sombatpraiwan

The Center for Plant Genetic Conservation Project Under the Royal Initiative of Her Royal Highness Princess Maha Chakri Sirindhorn of Suranaree University of Technology, Nakhon Ratchasima, Thailand

E-mail: rew40149@hotmail.com

ORCID id: https://orcid.org/0000-0003-1064-7652

Khongdet Phasinam*

Faculty of Engineering and Technology, Shinawatra University, Pathum Thani, Thailand

https://orcid.org/0000-0002-5795-9779

*Corresponding author e-mail: khongdet.p@siu.ac.th

ABSTRACT

This study aimed to investigate the phytochemical composition of different parts of Radermachera ignea and to evaluate its potential as a natural dye source for cotton and silk with enhanced wash and light fastness. Phytochemical screening of bark, leaves, and flowers was conducted using standard qualitative assays, while dye extraction from fresh and withered flowers was performed using aqueous and ethanol solvents (25–95%). Dyeing experiments incorporated natural and metal mordants, followed by colorimetric evaluation (L*, a*, b* system). Wash fastness was assessed using simulated ultrasonic washing with sodium lauryl sulfate, and light fastness was evaluated under UVC irradiation to accelerate photodegradation. Results revealed that bark extracts were rich in flavonoids and anthraquinones, while leaves showed high levels of saponins and steroids. Flowers contained significant terpenoids and reducing sugars. Statistical analysis (ANOVA and Duncan test) demonstrated significant differences (p < 0.05) in color properties across extraction methods and mordant treatments. Withered flower extracts obtained using 75% ethanol produced superior dyeing performance. Natural mordants such as tea leaves and banana sap enhanced red coloration and improved durability, while metal mordants (copper and iron) significantly increased yellow tones and color stability after washing and UV exposure. In conclusion, R. ignea flowers represent a promising sustainable natural dye source, with optimized extraction and mordanting strategies significantly improving textile color quality and fastness. This study also introduces a novel approach for standardizing metal mordant application based on central ion concentration, contributing to advancements in eco-friendly textile processing.

Keywords: Radermachera ignea, Phytochemical screening, Natural dye, Wash fastness, Light fastness

INTRODUCTION

The Radermachera ignea (RI) (Kurz) Steenis (synonym: Mayodendron igneum (Kurz) Kurz), the emblem tree of Suranaree University of Technology. It is found distributed in dry evergreen and mixed deciduous forests in southern China, Vietnam, Laos, Thailand, and Myanmar, at altitudes of 500–1000 meters above sea level, and produces bright orange flowers.

This research will be divided into two parts: 1) preliminary examination of phytochemicals in the bark, leaves, and flowers of the RI tree. and 2) This study investigated the effects of natural tannins, metal salts, or natural tannins combined with metal salts on the color fastness of cotton and silk dyed using extracts from the RI tree. The dyes were then tested with ultrasonic washing and UV explosion.

In the bark of the RI tree, Guo et al. (2007) extracted with 95% ethanol and continued sequential extraction, reporting 19 compounds grouped into phenolic compounds, chromones, monoterpenes, diterpenes, triterpenes, amides, and anthraquinones. Hashem et al. (2007) used petroleum ether, chloroform, ethyl acetate, and 95% ethanol, followed by purification using various solvents and techniques for leaf extraction. Five compounds were isolated, consisting of flavonoids such as flavone and isoflavones. Hashem et al. (2012) began extraction of leaves with 80% ethanol, followed by purification using other solvents and techniques. Five compounds were found, which could be grouped into sterols, diterpenes, and triterpenes. And Shabana et al. (2013) used 80% ethanol for leaf extraction, then using other solvents and techniques to aid in purification. The compounds could be grouped into flavonoids and coumarins. Sompong and Trakanrungroj (2010) extracted and analyzed compounds in the RI flowers. The extraction began with 90% methanol, followed by purification using other solvents and techniques. They found that the pigment from the RI tree flower is β, β -carotene-3,3’-diol or zeaxanthin, which is a xanthophyll. They also found two steroid compounds, β -sitosterol and stigmasterol, in the RI flower.

However, the reports found focus on detailed identification of pure compounds in depth; no reports on the overall composition of different parts of the RI tree have been found.	Furthermore, it can be seen that various reports begin the extraction process using organic solvents with low or moderate polarity. Therefore, plant compounds that are more polar than the first type of solvent are filtered out from the start. This experiment therefore proposes solvent extraction methods within the appropriate range for each group of compounds to be studied.  The details will be explained in the material and methods.

Subsequently, another part of the research will study the extraction of RI flower extract to test its dyeing properties on cotton and silk fibers, and test its wash resistance by simulating ultrasonic washing, as well as its light resistance using short-wave UV radiation. Dyeing generally involves the use of mordants, particularly metal salts, whose quantities can be precisely calculated because high-purity chemicals are used. Generally, there are two methods of application: 1) specifying the concentration of the mordant solution as %w/v in the volume of the dye solution, and 2) specifying it as % weight of the chemical including the water of crystallization on weight fiber (o.w.f.).

However, the atomic weights of the central metallic atoms in complexes vary, and each compound contains the weights of other elements, even the weight of water of crystallization, such as CuSO45H2O, FeSO47H2O and KAl(SO4)212H2O. The total weight used is expressed as %w/v in dye volume or % on weight fiber. The amount of central metal ions dissolved in the dye for each type of fabric varies and can differ significantly. This quantity of central metal atom ions is the actual substance used to immobilize the fibers to create a complex, which is the primary purpose of using mordant.

Therefore, this research presents a method for quantifying all types of copper, iron and aluminium ions, calculating to obtain 0.004 M ions. When dyeing, prepare 1,000 g of bleached cotton or silk fiber tassels in 25 mL of dye solution (material-to-liquor ratio, MLR  = 1:25). Theoretically, each piece of fabric would be treated with an equal amount of the central metal atom ion, either Cu, Fe, or Al, namely 0.0001 x the number of ions of the substance in 1 mole, or 6.02 x 1019 ions per gram of fiber.

To the best of my knowledge, there have been no published data on this concept. This could be described as introducing a novel principle for using mordants to calculate the theoretically equivalent number of central metal atom ions on weight of the fiber for metal ion mordants used in textile dyeing. Even in practical terms, it's impossible to create ideal conditions for every task, even in this research. However, this research was conducted based on this principle.

However, for natural mordants, the quantity cannot be precisely calculated, unlike the use of chemical metal salt mordants. Thus, the natural mordants were conducted using traditional methods: weighing dried tea leaves, dried licorice root, or dried pomegranate peel, grinding them, sieving them, weighing the mass, boiling them with water, filtering, and adjusting the volume.

Wash Fastness Testing Using Simulated Ultrasonic Washing

Because wash resistance testing focuses on two main factors: 1) the detergent solution used, with Sodium Lauryl Sulfate (SLS) being used as a representative detergent because it is the main component found in currently used cleaning agents, and 2) physical factors such as temperature and mechanical force.

Using ultrasonic waves, mechanical force is generated through vibrations in a medium. This creates the phenomenon of rapidly collapsing and expanding air cavities or ultrasonic cavitation, generating physical forces that can be used to simulate washing conditions in a test tube.

Light Fastness Testing Using Short-Wave Ultraviolet Radiation

Photodegradation is a process in which a material breaks down by absorbing energy from light. Generally, UV light is the primary light source that causes photodegradation. (Singh and Sharma, 2008, Wang et al. 2020, Ding et al., 2022) In particular, the primary wavelength range that initiates the light-induced degradation process is near-UV light, which spans from 290-400 nm. (Singh and Sharma, 2008; Dimassi et al., 2022)

This research uses UVC radiation to accelerate photochemical decay, based on the mechanism where photons collide with atoms or molecules, the atoms or molecules absorb energy, and the photon's energy is then transferred to electrons. If the energy supplied exceeds the binding energy, the bonds within the molecule are broken. This can occur through either heterolytic cleavage or homolytic cleavage, which produces free radicals as a product. (Montagna et al., 2018)

The removal of electrons from the sample molecule (photoionization) generates unstable and highly reactive free radicals. (De Jager et al., 2017; Wei et al., 2024) UVA and UVB also generate free radicals in a similar way, but UVC has higher energy. Based on the principle that shorter wavelengths of light generally provide higher energy, they accelerate photodegradation and increase the reaction rate. This principle is reflected in the degradation results of many organic dyes and pigments. (Jørgensen et al., 1991; Jespersen et al., 2005; Ahmad et al, 2006; Weyermann et al., 2006; Hattori et al., 2012; Groeneveld et al., 2023). The UVC radiation has an enormous oxidation potential; a 253.7 nm photon delivers 4.89 eV of energy, which is typically sufficient to interact with the electron structure of matter. (Da Silva and Faria, 2003)

This research therefore uses UVC, a short-wave ultraviolet radiation, as a representative of the UV light range to accelerate the aging process of light exposure. Although sunlight reaching the Earth's surface does not reach the UVC wavelength range due to absorption by the upper atmosphere, when the same conditions are applied to the samples in each treatment, If a treatment is susceptible to short-wave UV light—i.e., exhibits significant color changes from its original state—it can be assumed that such a treatment tends to have weaker color fastness than other treatments under sunlight conditions.

MATERIALS AND METHODS

The RI Tree is the official tree of Suranaree University of Technology (SUT). Its species has been verified and certified by the university's botany experts for several decades. These plant samples were collected from SUT campus, Nakhon Ratchasima, Thailand, in February 2025. The bark (outer layer extending to the cambium), middle-aged leaves, and fresh blooming flowers were collected, washed with RO water, dried at 40°C for 24 hours, and then ground and sieved through a 0.250 mm screen. Phytochemical analysis is pending. While the flowers used for dyeing cotton and silk are divided into two groups: those that are freshly bloomed and still attached to the tree or have just fallen but are still fresh, and those that have withered and turned dark but are not yet dry.

The dried tea leaves used were commercially available Three Horses brand. Dried licorice root and pomegranate peel were obtained from Kui Lim Hung Co., Ltd. Banana sap was obtained from banana floral inflorescence within the farm campus.

The cotton threads are raw, twisted cotton from Chiang Mai province. The silk threads are degummed silk from Chul Thai Silk Co., Ltd. in Phetchabun province.

Part of plant were collected from RI tree in February 2025. The bark, mid-mature leaves, and fresh blooming flowers were collected, washed with RO water, dried at 40°C for 24 hours, and then finely ground. Extraction was performed using aqueous-ethanol solutions appropriate to the range of compounds.

Phytochemical Screening

Each plant powder was immersed in a solvent (5g:100mL) at room temperature, stirred with a magnetic stirrer for 6 hours. The solvents chosen for this experiment: tannins and phlobatannins were water; Saponins, flavonoids, and anthraquinones were extracted using 65% EtOH. Coumarins and triterpenoids were extracted using 75% EtOH. Steroids, including deoxysugars which are components of cardiac glycosides, were extracted using 85% EtOH.   Next, the sample was placed in a 40kHz 300W ultrasonic bath and exposed to waves for 30 minutes at 30°C. It was then filtered through Whatman No. 1 filter paper, and a vacuum evaporator was used to separate the solvent. The crude extract was collected and tested.

The following testing methodology is modified based on the following principles from Evans (2009), Ben et al. (2013), Quraishi (2016), Gul et al. (2017), Narakornwit et al (2018), Shaikh and Patil (2020), Dubale et al. (2023) and Taesotikul et al. (2023)

1) For tannin testing, Ferric chloride test: weigh 0.2 g of the crude extract obtained from water extraction, add 5.0 ml of distilled water, and heat on a water bath for 5 minutes. Filter the liquid. Add 5 drops of ferric chloride solution (1% FeCl3) to the filtered liquid. Shake. If a greenish-black or bluish-black solution appears, tannins are present. Lead acetate test: To 1 ml aliquot of each of the extracts, 10 ml of water and 5 drops of 1% lead acetate solution was added. The formation of white precipitate indicated the presence of tannins.

Gelatin test: To about 1 g of each of the extracts, 1% gelatin solution containing sodium chloride was added. Formation of white precipitate indicated the presence of tannins (Tiwari et al., 2011).

2) For the flabatannin test, weigh 0.2 g of the crude extract obtained from water extraction, add 5.0 ml of distilled water, heat on a steam bath for 5 minutes, and filter. Add a hydrochloric acid solution (10% HCl) to the filtered liquid, shake, and heat over a water bath for 5 minutes. If the solution turns red, it indicates the presence of phlobatannin.

3) For saponin testing, weigh 0.2 g of the crude extract obtained through 65% EtOH extraction, add 5.0 ml of distilled water, heat on a water bath for 5 minutes, and shake vigorously. Observe the collapse of the bubbles after 15 minutes, if permanent bubbles remain or are difficult to collapse after more than 15 minutes, it indicates the presence of saponin.

4) For the flavonoid test, weigh 0.2 g of the crude extract from 65% EtOH, dissolve in 5.0 ml of 65% ethanol, shake, and filter. For the first test, place the magnesium piece into filtered solution and add a few drops of concentrated hydrochloric acid. (Shinoda’s test or cyanidin test), For the second test, place a small piece of zinc metal into filtered solution and drop concentrated hydrochloric acid (Pew's test), shake, and then heat it over a water bath for 5 minutes. If the solution turns pink-red, it indicates the presence of flavonoids. The sodium hydroxide solution test yields a positive result when it turns yellow-brown or red. The concentrated sulfuric acid test yields a positive result when it turns pink-red. The Rao and Sheshadri test with concentrated nitric acid produces a blue color, and the final method involves testing with boric acid and adding 2-3 drops of acetic acid, resulting in a yellow color and green fluorescence.

5) For the anthraquinone test, weigh 0.2 g of the crude extract from 65% EtOH. Add 5 ml of 10% H2SO4 solution, shake, heat on a water bath for 5 minutes, filter, allow the solution to cool to room temperature and extract with chloroform 5 ml. Add 3 ml of ammonia solution (10% NH3). If a pinkish-red color appears in the solution, anthraquinone is present.

6) For coumarin testing, weigh 0.2 g of the crude extract obtained from extraction with 75% EtOH, dissolve it in 5.0 ml of 75% ethanol, shake, and filter out the insoluble portion. Add sodium hydroxide solution (6 M NaOH) to the filtered liquid. If the solution turns dark yellow, it indicates the presence of coumarin, but this needs to be confirmed by UV fluorescence at a wavelength of 365 nanometers.

7) For triterpenoid testing, weigh 0.2 g of the crude extract obtained through 75% EtOH extraction, dissolve it in 5 ml of chloroform, shake, and filter out the insoluble portion. Slowly add concentrated sulfuric acid to the resulting liquid. If a brown ring appears at the interface between the extract layer and the sulfuric acid layer, it indicates the presence of triterpenoids.

8) For the Liebermann-Burchard steroid test, weigh 0.2 g of the crude extract obtained from 85% EtOH extraction, dissolve in 5 ml of chloroform, shake, and filter out the undissolved portion. Take the filtered liquid, add glacial acetic acid, shake, and then add concentrated sulfuric acid. If the solution appears blue or bluish-green, it indicates the presence of steroids. However, if it appears red, orange, or purple, it means the substance contains triterpenoids.

9) To test for deoxy-sugar using the Keller-Kiliani (KK) test, weigh 0.2 g of the crude extract obtained from extraction with 85% EtOH, dissolve it in 5 ml of chloroform, and filter out the undissolved portion. Add ferric chloride solution (1% FeCl3) to the filtered liquid, shake, add glacial acetic acid, shake, and gradually add concentrated sulfuric acid. If a brown ring appears at the interface between the extract layer and the sulfuric acid layer, it indicates the presence of deoxysugar.

10) For the reducing sugar test (Benedict's test), prepare Benedict's solution from 4.325 g of copper sulfate pentahydrate, 43.25 g of sodium citrate, and 25 g of sodium carbonate, dissolved in distilled water to a total volume of 500 mL. The test is performed by reacting an aqueous extract from a part of the plant with a 1:2 V/V Benedict's solution, heated for 3-5 minutes. A positive result shows a brick-red precipitate.

Extraction, Mordanting and Dyeing.

For natural mordants, weigh dried tea leaves, dried licorice root, or dried pomegranate peel. Grind through a 1 mm sieve. Extract with 3 g/L of water, 50°C. (Gironi and Piemonte, 2011; Lambrecht, et al., 2023) 120 min (Lambrecht, et al., 2020; Lambrecht, et al., 2023) Filter and use. For banana sap mordant, use 20 mL/L of banana sap.

For metal mordants, AR grade of CuSO45H2O (Loba Chemie), FeSO47H2O (Carlo Erba) and KAl(SO4)212H2O (Loba Chemie) were calculated to obtain central metal ions to 0.004 M for create a complex of each when dyeing by preparing 1.000 grams of bleached cotton or silk tassels.

For the extraction of RI flower, two groups of RI flowers were selected: flowers that were withered and turned dark orange or brown (d-), and flowers that were blooming on the tree or had just fallen but were still fresh (f-). Each group was dried at 45°C for 12 hours, ground through a 1 mm sieve, and the color was extracted using water (-w) and ethanol -25, 50, 75, and 95% as solvents. The ratio of RI flower powder to solvent was 1:20 W/V. The mixture was then heated in a water bath shaker at 50°C for 120 minutes (Lambrecht et al., 2023), filtered.

Mordant treatments include the following: (1) no mordant, (2) tea leaves, (3) banana sap, (4) licorice root, (5) pomegranate fruit peel, (6) copper solution, (7) iron solution, (8) aluminum solution, (9) tea/copper, (10) tea/iron, (11) tea/aluminum, (12) banana sap/copper, (13) banana sap/iron, (14) banana sap/aluminum, (15) licorice/copper, (16) licorice/iron, (17) licorice/aluminum, (18) pomegranate/copper, (19) pomegranate/iron and (20) pomegranate/aluminum.

The single mordants were used to stain sample 2) to 8). Mordant application was prior to dyeing (pre-mordanting) at MLR of 1:25 W/V 50°C 90 min in water bath shaker. Dry in the shade for 2 days. Then, it was dyed with color from RI flowers at a temperature of 50°C (Lambrecht, et al., 2023) for 120 minutes in water bath shaker.

In case of using natural mordant combined with metal mordant. The process is carried out by pre-mordanting by natural mordant 50°C 45 minutes. Dry in the shade for 2 days. Then, it was dyed with color from RI flowers at a temperature of 50°C for 120 minutes. Dry in the shade for 2 days, then post-mordanting in a metal mordant solution, reduced to half its concentration, at 50°C for 45 minutes. Both mordanting and dyeing use MLR of 1:25 W/V.

The fabrics are then rinsed under running tap water for 3 minutes, wrung out, and dried at 40°C for 12 hours. Colorimetric measurements (L*, a*, b*) were performed using the Hunter Lab UltraScan VIS colorimeter. Current Sensor: Ultrascan VIS “UVVIS2608”. The measurement used D65 light, a 0.375” area of ​​view, and the Reflectance Specular Excluded mode. One batch of dyed cotton and silk is then washed and color measured, while another batch is exposed to UV light and color measured again.

1) Wash fastness testing using simulated ultrasonic washing

The test used a ultrasonic cleaner, a Cole-Palmer Model 08895-19, with a wave frequency of 40kHz and a power of 300W, to simulate washing. 1.0 g of each treated dyed fiber tassel was immersed in a 2000 ppm (2g/L) solution of Sodium lauryl sulfate AR grade (Loba Chemie) with a volume of 25 mL/tube. Place the test tubes in a sieve, 50 tubes at a time, into the ultrasonic bath. Preheat the system to 30°C, then immerse the tubes for 10 minutes to allow the solution inside to reach 30°C. Next, immerse the tube rack in a ultrasonic bath for 30 minutes, then remove and rinse each fiber tassel under running tap water for 3 minute. Dry at 40°C for 12 hours and then measure the color.

2) Light fastness testing using short-wave ultraviolet radiation

This research used UVC as a representative light wave to test the lightfastness of fibers dyed with different treatments. The irradiation was performed using a PHILIPS, TUV 36W SLV/6 UVC lamp panel, Made in Poland, product code 871150061854210, two 120 cm long T8 tubes are used, each consuming 36 W of power and emitting a specified UVC of 16.4 W. The peak primary light wavelength is 253.7 nm. Each tube is placed parallel to the others, 20 cm apart. The perpendicular distance from the tube to the workpiece is 20 cm. The temperature and relative humidity in the laboratory are controlled at 25°C 65±5%R.H. The dyed fiber tassels were irradiated for 24 consecutive hours. The UV light unit and sample panels were installed in a blower to minimize ozone buildup, as it is an emerging interfering parameter that is outside the consideration of the lightfastness effect of fabric colors by short-wave UV radiation, color measurements are taken.

The L*, a*, and b* color data were processed using IBM SPSS Statistics V21.0. Statistical differences were identified using One-Way ANOVA (Analysis of Variance), and Duncan post-hoc tests were performed to test for homogeneity of variance. Factors considered included the condition of the RI flower when harvested (wilted or fresh) extraction with different solvents, and different mordant treatments.

RESULTS AND DISCUSSION

The results of phytochemical testing in different parts of the RI tree vary. For brevity, the information is presented in the following table.
Table 1: Phytochemical screening in the bark, leaves, and flowers of the RI Tree

| Group of phytochemical | Test method | Part of RI tree |  |  |
| --- | --- | --- | --- | --- |
|  |  | Bark | Leaves | Flower |
| Tannins | FeCl3 test-Braymer’s test | ++ | ++ | ++ |
|  | Lead sub acetate test | + | ++ | ++ |
|  | Gelatin test | + | + | + |
| Phlobatannins | HCl test | - | - | - |
| Saponins | Foam test | + | +++ | - |
| Anthraquinones | Borntrager’s test | +++ | - | - |
| Flavonoids | Shinoda’s test (Cyanidin test)/ Mg-HCl reduction test | +++ | + | - |
|  | Pew’s test /Zinc-HCl reduction test | - | - | - |
|  | Aqueous NaOH test | +++ | ++ | + |
|  | Sulfuric acid test | - | +/- | - |
|  | Rao and Sheshadri test (Nitric acid) | - | +/- | - |
|  | Boric acid + Acetic acid, (UV) | - | - | - |
| Coumarins | NaOH test, (UV) | +/- | ++ | ++ |
| Triterpenoids | Salkowski and Liebermann-Burchard’s tests | + | ++ | +++ |
| Steroids | Libermann-Burchard’s test | + | +++ | ++ |
| Deoxy sugars | Keller-Kiliani test | + | +++ | ++ |
| Reducing sugars | Benedict’s test | + | + | +++ |

- This means a negative result, which means the substance may be absent or present in such small quantities that the difference from the control cannot be observed.

+/- The report shows unclear results

+ detects and displays a slightly positive result

++ It was detected and the result is clearly positive.

+++ It was detected and the result is highly positive result.

Phytochemical analysis of the bark of the RI tree revealed tannins or polyphenols and flavonoids, consistent with the work of Guo et al. (2007). They found naringenin, quercetin, and naringin, which are both polyphenols and also have flavonoid structures. Furthermore, the bark of RI also showed positive results in triterpenoid, anthraquinone, and sterol tests, consistent with the analytical chemistry work of Guo et al. (2007); Phytochemical tests on the leaves of the RI Tree revealed the presence of flavonoids, consistent with the work of Hashem et al. (2007) and Shabana et al. (2013). Triterpenoids and sterols were also found in leaves, consistent with Hashem et al. (2012); The test results found steroids or phytosterols in the RI flower, consistent with the work of Sompong and Trakanrungroj (2010), who reported the presence of β-sitosterol and stigmasterol in the RI flower.

Analysis of variance (ANOVA) of cotton and silk fiber treatments showed that type of RI flower extracts yielded statistically significant differences in L*, a*, and b* dyeing values (Table A1 and A2). When the dyed fibers were analyzed using total variance to compare the color values ​​between mordants, statistically significant differences were found in ANOVA values ​​for L*, a*, and b* in both cotton and silk dyeing.  (Table A3 and A4) Specifically, each treatment yielded statistically significant differences in staining outcomes.

The results of the analysis of variance of color values ​​on cotton and silk fibers under the influence of RI flower extract after ultrasonic simulated washing. It was found that the mean color values ​​of L*, a*, and b* differed significantly (Table A5 and A6). When comparing the results of the ANOVA of color values ​​on cotton and silk fibers from the influence of mordant after simulation washing, it was found that the mean color values ​​for L*, a*, and b* differed significantly statistically. (Table A7 and A8)

Analysis of color variation on cotton and silk fibers under the influence of RI flower extract after photosensitivity testing using short-wave UV accelerated conditions. It was found that the mean color values ​​for L*, a*, and b* differed significantly statistically (Table A9 and A10). When comparing the results of ANOVA of color values ​​on cotton and silk fibers under the influence of mordants after irradiation with short-wave UV radiation. It was found that the mean color values ​​for L*, a*, and b* differed significantly statistically (Table A11 and A12).

However, when analyzing the data after post-hoc tests to test the homogeneity of variance to find the statistical classification of subsets that show the highest levels of red and yellow color on cotton and silk fibers. The obtained data can be presented in a summary table of recommendations for selecting RI extract and mordant as follows:

Table 2: The recommendations Duncan statistical classification of subsets for selecting RI flower extracts and mordants as follows

| Process | Fiber | Statistical classification of subsets | Factor: flower extracts | Factor: mordants |
| --- | --- | --- | --- | --- |
| Dyed | cotton | Most red value | d75 | (2) tea leaves |
|  |  | Most yellow value | d75, f75 | (6) copper solution, (7) iron solution |
|  | silk | Most red value | d50, d75 | (2) tea leaves, (3) banana sap |
|  |  | Most yellow value | dw, d25, d75 | (6) copper solution, (7) iron solution |
| After US simulation washing | cotton | Most red value | d75 | (3) banana sap |
|  |  | Most yellow value | d75, f75 | (16) licorice/iron sol. |
|  | silk | Most red value | dw, d50, d75 | (2) tea leaves |
|  |  | Most yellow value | dw, d25, d75 | (6) copper solution, (7) iron solution |
| After UV radiation testing. | cotton | Most red value | d75 | (3) banana sap |
|  |  | Most yellow value | d25, d75, d95, f75 | (6) copper solution |
|  | silk | Most red value | f25, f50, f95 | (2) tea leaves, (3) banana sap |
|  |  | Most yellow value | f25, f50, f75, f95 | (6) copper solution |

1    Flower extractive include the following: d- is dried or withered flora, f- is fresh; -w, 25, 50, 75 95 is extracted by water, 25, 50, 75 and 95% ethanol, respectively

2    Mordant treatments include the following: (1) no mordant, (2) tea leaves, (3) banana sap, (4) licorice root, (5) pomegranate fruit peel, (6) copper solution, (7) iron solution, (8) aluminum solution, (9) tea/copper, (10) tea/iron, (11) tea/aluminum, (12) banana sap/copper, (13) banana sap/iron, (14) banana sap/aluminum, (15) licorice/copper, (16) licorice/iron, (17) licorice/aluminum, (18) pomegranate/copper, (19) pomegranate/iron and (20) pomegranate/aluminum.

Conclusion

Preliminary phytochemical analysis of the bark of the RI revealed highly positive results for flavonoids and anthraquinones. Tannins showed a clearly positive result, while saponins, triterpenoids, steroids, deoxygenated sugars, and reducing sugars showed only slightly positive results.; The RI leaves showed highly positive results for saponins, steroids, and deoxygenated sugars. Tannins, flavonoids, coumarins, and triterpenoids showed clearly positive results. And reducing sugars showed a slightly positive result.; And in RI flowers, triterpenoids and reducing sugars were found, showing a highly positive result. Tannins, coumarins, steroids, and deoxygenated sugars were found to show clear positive results. However, flavonoids showed only a slightly positive result. However, the test results obtained are preliminary results of the crude extract under the experimental limits specified in the test conditions and methods. For accuracy or identification, the extract should be purified and analyzed using advanced instruments such as HPLC, LC-MS. Because orange is an iconic color of the RI flower, the goal is to achieve the orange color that is most effectively a combination of red and yellow. To improve wash and lightfastness in cotton, d75 flower extract and banana sap mordants, licorice/iron or copper sulfate can be used. For silk, to achieve the best possible orange color retention after washing, either dw or d75 flower extract can be used. However, for superior lightfastness, choose f25, f50, or f95. For mordants that can make silk resistant to washing and light, tea leaves and copper sulfate can be used.

Conflict of Interest

The authors declare no conflict of interest.

REFERENCES

Guo, H., Li, B.G., Qi, H.Y., & Zhang, G.L. (2007). A new meroditerpenoid from Mayodendron igeum. Journal of Asian Natural Products Research, 9(1): 1–5. https://doi.org/10.1080/10286020500289311

Hashem, F.A., El-Sawi, S.A., & Sleem, A.A. (2007). Phenolic compounds and bioactivity of leaves of Mayodendron igneum Kurz. Afr J Trad CAM, 4(3): 306–312.

Hashem, F.A., Sengab, A., Shabana, M., & Khaled, S. (2012). Antioxidant activity of Mayodendron igneum Kurz and the cytotoxicity of the isolated terpenoids. Journal of Medicinally Active Plants, 1: 88–97.

Shabana, M.H., Hashem, F.A., Singab, A.N., Khaled, S., & Farrag, A.R. (2013). Protective and therapeutic activities of Mayodendron igneum Kurz against paracetamol induced liver toxicity in rats and its bioactive constituents. Journal of Applied Pharmaceutical Science, 3(7): 147–155. https://doi.org/10.7324/JAPS.2013.3728

Sompong, D., & Trakanrungroj, P. (2010). The flower of Radermachera ignea (kurz) steenis, a new source of zeaxanthin. Suranaree J Sci Technol, 17: 303–308.

Singh, B., & Sharma, N. (2008). Mechanistic implications of plastic degradation, Polymer Degradation and Stability. 93(3): 561–584. https://doi.org/10.1016/j.polymdegradstab. 2007.11.008

Wang, C., Zeyu, X., Xin, J., Sijia, L., Zhanghao C., Bo P., Bing W., Yong, S.O., & Cheng, G., (2020). Photo-aging of polyvinyl chloride microplastic in the presence of natural organic acids. Water Research, 183: 116082. https://doi.org/10.1016/j.watres.2020.116082

Ding, L., Yu, X., Guo, X., Zhang, Y., Ouyang, Z., Liu, P., Zhang, C., Wang, T., Jia, H., & Zhu, L. (2022). The photodegradation processes and mechanisms of polyvinyl chloride and polyethylene terephthalate microplastic in aquatic environments: Important role of clay minerals, Water Research, 208: 117879. https://doi.org/10.1016/j.watres.2021. 117879

Dimassi, S.N., Hahladakis, J.N., Yahia, M.N.D., Ahmad, M.I., Sayadi, S., & Al-Ghouti, M.A. (2022). Degradation-fragmentation of marine plastic waste and their environmental implications: A critical review. Arabian Journal of Chemistry, 15: 104262. https:// doi.org/10.1016/j.arabjc.2022.104262

Montagna, L.S., Montanheiro, T.L.D.A., Borges, A.C., Koga‐Ito, C.Y., Lemes, A.P., Rezende M.C. (2018). Influence of photodegradation with UV radiation in biotreatment with Paecilomyces variotti on PHBV/GNS nanocomposites. IET Nanobiotechnol. 12: 285–291. https://doi.org/10.1049/iet-nbt.2017.0020

De Jager, T.L., Cockrell, A.E., Du Plessis, S.S. (2017). Ultraviolet Light Induced Generation of Reactive Oxygen Species. Advances in Experimental Medicine and Biology, 996: 15–23. https://doi.org/10.1007/978-3-319-56017-5_2

Wei, M., He, X., Liu, N., & Deng, H. (2024). Role of reactive oxygen species in ultraviolet-induced photodamage of the skin. Cell Division, 19: 1. https://doi.org/10.1186/s13008-024-00107-z

Jørgensen, K., & Skibsted, L.H. (1991). Light sensitivity of cochineal. Quantum yields for photodegradation of carminic acid and conjugate bases in aqueous solution. Food Chemistry, 40(1): 25–34. https://doi.org/10.1016/0308-8146(91)90016-H

Jespersen, L., Strømdahl, L.D., Olsen, K., & Skibsted, L.H. (2005). Heat and light stability of three natural blue colorants for use in confectionery and beverages. European Food Research and Technology, 220: 261–266. https://doi.org/10.1007/s00217-004-1062-7

Ahmad, I., Fasihullah, Q., & Vaid, F.H.M. (2006). Effect of light intensity and wavelengths on photodegradation reactions of riboflavin in aqueous solution. Journal of Photochemistry and Photobiology B: Biology, 82(1): 21–27. https://doi.org/10.1016/j.jphotobiol.2005.08.004

Weyermann, C., Kirsch, D., Costa-Vera, C., & Spengler, B. (2006). Photofading of ballpoint dyes studied on paper by LDI and MALDI MS. Journal of the American Society for Mass Spectrometry, 17(3): 297–306. https://doi.org/10.1016/j.jasms.2005.11.010

Hattori, H., Yoshizumi, K., & Crews, P.C. (2012). Wavelength sensitivity of AATCC Blue wool lightfastness standards under light radiation. Dyes and Pigments, 92(3): 936–941. https://doi.org/10.1016/j.dyepig.2011.05.015

Groeneveld, I., Kanelli, M., Ariese, F., & van Bommel, M.R. (2023). Parameters that affect the photodegradation of dyes and pigments in solution and on substrate – An overview, Dyes and Pigments, 210: 110999. https://doi.org/10.1016/j.dyepig.2022.110999

Da Silva, C.G., & Faria, J.L. (2003). Photochemical and photocatalytic degradation of an azo dye in aqueous solution by UV irradiation, Journal of Photochemistry and Photobiology A: Chemistry, 155 (1–3): 133–143. https://doi.org/10.1016/S1010-6030(02)00374-X

Evans. (2009). Trease and Evans Pharmacognosy. 16th edition. Saunders Elsevier.

Ben, I.O., Woode, E., Abotsi, W.K.M., & Boakye-Gyasi, E. (2013). Preliminary phytochemical screening and in vitro antioxidant properties of Trichilia monadelpha (Thonn.) J. J. de Wilde (Meliaceae). Journal of Medical and Biomedical Sciences, 2(2): 6–15

Quraishi, R.K.Y.K. (2016). Macromorphological, anatomical studies and flavonoid estimation of Ipomoea aquatica Forssk. and Argyreia nervosa (Burn.f.). Int. Res. Journal of Science & Engineering, 4(1): 43-47.

Gul, R., Jan, S.U., Faridullah, S., Sherani, S., & Jahan, N. (2017). Preliminary Phytochemical Screening, Quantitative Analysis of Alkaloids, and Antioxidant Activity of Crude Plant Extracts from Ephedra intermedia Indigenous to Balochistan, The Scientific World Journal, 5873648. https://doi.org/10.1155/2017/5873648

Narakornwit, W., Sukwattanasinit, T., Wangwattana, B., Srisopon, S., Burana-osot, J. & Sotanaphun, U. (2018). Discrimination of botanical origin of Chan-thet, Chan-hom, Chan-chamot, Chan-khao and Chan-thana using chemical test and thin-layer chromatography. Thai Pharmaceutical and Health Science Journal, 13(3): 142–149.

Shaikh, J.R., & Patil, M.K. (2020). Qualitative tests for preliminary phytochemical screening: An overview. International Journal of Chemical Studies, 8(2): 603–608. https://doi.org/10.22271/chemi.2020.v8.i2i.8834

Dubale, S., Kebebe, D., Zeynudin, A., Abdissa, N., & Suleman, S. (2023). Phytochemical screening and antimicrobial activity evaluation of selected medicinal plants in Ethiopia. Journal of Experimental Pharmacology, (15): 51–62. https://doi.org/10.2147/JEP.S379805

Taesotikul, T., Kitcharoen, N., Chinpaisal, C., Phuagphong, P., & Nawanopparatsakul, S. (2023). Extraction and analyses of phytochemical compounds from Citrus hystrix peels for molluscicidal activities. Thai Bulletin of Pharmaceutical Sciences, 18(1): 17–28. https://doi.org/10.69598/tbps.18.1.17-28

Gironi, F., & Piemonte, V. (2011). Temperature and solvent effects on polyphenol extraction process from chestnut tree wood. Chemical Engineering Research and Design, 89(7), 857–862. https://doi.org/10.1016/j.cherd.2010.11.003

Lambrecht, L., Gisbert-Payá, J., Bou-Belda, E., & Bonet, M.Á. (2020). Optimization of tea extracts composition to dye cotton. Time and temperature influence. Journal of Applied Research in Technology & Engineering, 1(1): 3–7. https://doi.org/10.4995/jarte.2020.13480

Lambrecht, L., Capablanca, L., Bou-Belda, E., Montava, I., Díaz-García, P., & Gisbert-Payá, J. (2023). Enhancing polyphenols and tannins concentration on cotton dyed with red tea. Sustainability, 15, 3062. https://doi.org/10.3390/su15043062

Appendix

Table A1: Analysis of the total variance of the mean L*, a*, and b* color values ​​on cotton fibers after dyeing to compare the influence of different flower extracts

| ANOVA |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  | Sum of Squares | df | Mean Square | F | Sig. |
| lightness | Between Groups | (Combined) |  | 3018.865 | 9 | 335.429 | 11.388 | .000 |
|  |  | Linear Term | Contrast | 392.430 | 1 | 392.430 | 13.323 | .000 |
|  |  |  | Deviation | 2626.435 | 8 | 328.304 | 11.146 | .000 |
|  | Within Groups |  |  | 29159.686 | 990 | 29.454 |  |  |
|  | Total |  |  | 32178.551 | 999 |  |  |  |
| redness | Between Groups | (Combined) |  | 272.811 | 9 | 30.312 | 14.182 | .000 |
|  |  | Linear Term | Contrast | 1.557 | 1 | 1.557 | .729 | .394 |
|  |  |  | Deviation | 271.254 | 8 | 33.907 | 15.864 | .000 |
|  | Within Groups |  |  | 2116.019 | 990 | 2.137 |  |  |
|  | Total |  |  | 2388.830 | 999 |  |  |  |
| yellowness | Between Groups | (Combined) |  | 1817.389 | 9 | 201.932 | 31.401 | .000 |
|  |  | Linear Term | Contrast | 77.067 | 1 | 77.067 | 11.984 | .001 |
|  |  |  | Deviation | 1740.322 | 8 | 217.540 | 33.829 | .000 |
|  | Within Groups |  |  | 6366.345 | 990 | 6.431 |  |  |
|  | Total |  |  | 8183.733 | 999 |  |  |  |

Table A2: Analysis of the total variance of the mean L*, a*, and b* color values ​​on silk fibers after dyeing to compare the influence of different flower extracts

| ANOVA |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  | Sum of Squares | df | Mean Square | F | Sig. |
| lightness | Between Groups | (Combined) |  | 4779.555 | 9 | 531.062 | 11.930 | .000 |
|  |  | Linear Term | Contrast | 3059.294 | 1 | 3059.294 | 68.724 | .000 |
|  |  |  | Deviation | 1720.262 | 8 | 215.033 | 4.830 | .000 |
|  | Within Groups |  |  | 44070.659 | 990 | 44.516 |  |  |
|  | Total |  |  | 48850.215 | 999 |  |  |  |
| redness | Between Groups | (Combined) |  | 238.985 | 9 | 26.554 | 13.110 | .000 |
|  |  | Linear Term | Contrast | 88.783 | 1 | 88.783 | 43.832 | .000 |
|  |  |  | Deviation | 150.202 | 8 | 18.775 | 9.269 | .000 |
|  | Within Groups |  |  | 2005.266 | 990 | 2.026 |  |  |
|  | Total |  |  | 2244.251 | 999 |  |  |  |
| yellowness | Between Groups | (Combined) |  | 1740.699 | 9 | 193.411 | 22.064 | .000 |
|  |  | Linear Term | Contrast | 997.817 | 1 | 997.817 | 113.830 | .000 |
|  |  |  | Deviation | 742.882 | 8 | 92.860 | 10.593 | .000 |
|  | Within Groups |  |  | 8678.182 | 990 | 8.766 |  |  |
|  | Total |  |  | 10418.880 | 999 |  |  |  |

Table A3: Analysis of the total variance of the mean color values ​​L*, a*, and b* on cotton fibers after dyeing to compare the influence of different mordants

| ANOVA - Dyed Cotton /Treatment |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  | SS | df | MS | F | Sig. |
| lightness | Between Groups | (Combined) |  | 37358.757 | 19 | 1966.250 | 328.651 | .000 |
|  |  | Linear Term | Contrast | 1755.559 | 1 | 1755.559 | 293.435 | .000 |
|  |  |  | Deviation | 35603.198 | 18 | 1977.955 | 330.608 | .000 |
|  | Within Groups |  |  | 5863.128 | 980 | 5.983 |  |  |
|  | Total |  |  | 43221.885 | 999 |  |  |  |
| redness | Between Groups | (Combined) |  | 810.367 | 19 | 42.651 | 69.055 | .000 |
|  |  | Linear Term | Contrast | 172.533 | 1 | 172.533 | 279.342 | .000 |
|  |  |  | Deviation | 637.834 | 18 | 35.435 | 57.372 | .000 |
|  | Within Groups |  |  | 605.287 | 980 | .618 |  |  |
|  | Total |  |  | 1415.654 | 999 |  |  |  |
| yellowness | Between Groups | (Combined) |  | 3871.395 | 19 | 203.758 | 56.504 | .000 |
|  |  | Linear Term | Contrast | 20.238 | 1 | 20.238 | 5.612 | .018 |
|  |  |  | Deviation | 3851.157 | 18 | 213.953 | 59.332 | .000 |
|  | Within Groups |  |  | 3533.934 | 980 | 3.606 |  |  |
|  | Total |  |  | 7405.329 | 999 |  |  |  |

Table A4: A total variance analysis of the mean L*, a*, and b* color values ​​on silk fibers after dyeing was performed to compare the influence of different mordants

| ANOVA - Dyed Silk /Treatment |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  | Sum of Squares | df | Mean Square | F | Sig. |
| lightness | Between Groups | (Combined) |  | 41510.556 | 19 | 2184.766 | 291.713 | .000 |
|  |  | Linear Term | Contrast | 1761.067 | 1 | 1761.067 | 235.140 | .000 |
|  |  |  | Deviation | 39749.489 | 18 | 2208.305 | 294.856 | .000 |
|  | Within Groups |  |  | 7339.658 | 980 | 7.489 |  |  |
|  | Total |  |  | 48850.215 | 999 |  |  |  |
| redness | Between Groups | (Combined) |  | 1271.712 | 19 | 66.932 | 67.446 | .000 |
|  |  | Linear Term | Contrast | 568.791 | 1 | 568.791 | 573.155 | .000 |
|  |  |  | Deviation | 702.921 | 18 | 39.051 | 39.351 | .000 |
|  | Within Groups |  |  | 972.538 | 980 | .992 |  |  |
|  | Total |  |  | 2244.251 | 999 |  |  |  |
| yellowness | Between Groups | (Combined) |  | 5530.935 | 19 | 291.102 | 58.364 | .000 |
|  |  | Linear Term | Contrast | 1006.844 | 1 | 1006.844 | 201.865 | .000 |
|  |  |  | Deviation | 4524.091 | 18 | 251.338 | 50.392 | .000 |
|  | Within Groups |  |  | 4887.945 | 980 | 4.988 |  |  |
|  | Total |  |  | 10418.880 | 999 |  |  |  |

Table A5: A total variance analysis of the mean L*, a*, and b* color values ​​on cotton fibers after simulated ultrasonic washing was performed to compare the influence of different flower extracts

| ANOVA |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  |  | Sum of Squares | df | Mean Square | F | Sig. |
| lightness | Between Groups | 1553.727 | 9 | 172.636 | 5.549 | .000 |
|  | Within Groups | 30802.622 | 990 | 31.114 |  |  |
|  | Total | 32356.349 | 999 |  |  |  |
| redness | Between Groups | 107.423 | 9 | 11.936 | 5.776 | .000 |
|  | Within Groups | 2045.643 | 990 | 2.066 |  |  |
|  | Total | 2153.066 | 999 |  |  |  |
| yellowness | Between Groups | 877.584 | 9 | 97.509 | 16.251 | .000 |
|  | Within Groups | 5940.078 | 990 | 6.000 |  |  |
|  | Total | 6817.662 | 999 |  |  |  |

Table A6: shows the overall analysis of variance of the mean L*, a*, and b* color values ​​on silk fibers after simulated ultrasonic washing, comparing the influence of different flower extracts

| ANOVA |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  |  | Sum of Squares | df | Mean Square | F | Sig. |
| lightness | Between Groups | 3944.008 | 9 | 438.223 | 11.045 | .000 |
|  | Within Groups | 39277.877 | 990 | 39.675 |  |  |
|  | Total | 43221.885 | 999 |  |  |  |
| redness | Between Groups | 124.161 | 9 | 13.796 | 10.575 | .000 |
|  | Within Groups | 1291.493 | 990 | 1.305 |  |  |
|  | Total | 1415.654 | 999 |  |  |  |
| yellowness | Between Groups | 1255.280 | 9 | 139.476 | 22.452 | .000 |
|  | Within Groups | 6150.049 | 990 | 6.212 |  |  |
|  | Total | 7405.329 | 999 |  |  |  |

Table A7: Analysis of the total variance of the mean color values ​​L*, a*, and b* on cotton fibers after simulated ultrasonic washing to compare the influence of different mordants

| ANOVA |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  | Sum of Squares | df | Mean Square | F | Sig. |
| lightness | Between Groups | (Combined) |  | 27621.056 | 19 | 1453.740 | 300.861 | .000 |
|  |  | Linear Term | Contrast | 363.058 | 1 | 363.058 | 75.137 | .000 |
|  |  |  | Deviation | 27257.998 | 18 | 1514.333 | 313.401 | .000 |
|  | Within Groups |  |  | 4735.293 | 980 | 4.832 |  |  |
|  | Total |  |  | 32356.349 | 999 |  |  |  |
| redness | Between Groups | (Combined) |  | 1765.900 | 19 | 92.942 | 235.256 | .000 |
|  |  | Linear Term | Contrast | 55.186 | 1 | 55.186 | 139.688 | .000 |
|  |  |  | Deviation | 1710.713 | 18 | 95.040 | 240.565 | .000 |
|  | Within Groups |  |  | 387.167 | 980 | .395 |  |  |
|  | Total |  |  | 2153.066 | 999 |  |  |  |
| yellowness | Between Groups | (Combined) |  | 4071.522 | 19 | 214.291 | 76.473 | .000 |
|  |  | Linear Term | Contrast | 28.619 | 1 | 28.619 | 10.213 | .001 |
|  |  |  | Deviation | 4042.903 | 18 | 224.606 | 80.154 | .000 |
|  | Within Groups |  |  | 2746.140 | 980 | 2.802 |  |  |
|  | Total |  |  | 6817.662 | 999 |  |  |  |

Table A8: shows the overall analysis of variance of the mean color values ​​L*, a*, and b* on silk fibers after simulated ultrasonic washing to compare the influence of different mordants

| ANOVA |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  | Sum of Squares | df | Mean Square | F | Sig. |
| lightness | Between Groups | (Combined) |  | 37358.757 | 19 | 1966.250 | 328.651 | .000 |
|  |  | Linear Term | Contrast | 1755.559 | 1 | 1755.559 | 293.435 | .000 |
|  |  |  | Deviation | 35603.198 | 18 | 1977.955 | 330.608 | .000 |
|  | Within Groups |  |  | 5863.128 | 980 | 5.983 |  |  |
|  | Total |  |  | 43221.885 | 999 |  |  |  |
| redness | Between Groups | (Combined) |  | 810.367 | 19 | 42.651 | 69.055 | .000 |
|  |  | Linear Term | Contrast | 172.533 | 1 | 172.533 | 279.342 | .000 |
|  |  |  | Deviation | 637.834 | 18 | 35.435 | 57.372 | .000 |
|  | Within Groups |  |  | 605.287 | 980 | .618 |  |  |
|  | Total |  |  | 1415.654 | 999 |  |  |  |
| yellowness | Between Groups | (Combined) |  | 3871.395 | 19 | 203.758 | 56.504 | .000 |
|  |  | Linear Term | Contrast | 20.238 | 1 | 20.238 | 5.612 | .018 |
|  |  |  | Deviation | 3851.157 | 18 | 213.953 | 59.332 | .000 |
|  | Within Groups |  |  | 3533.934 | 980 | 3.606 |  |  |
|  | Total |  |  | 7405.329 | 999 |  |  |  |

Table A9: Analysis of the total variance of the mean L*, a*, and b* color values ​​on cotton fibers after testing for lightfastness with short-wave UV irradiation, comparing the influence of different flower extracts

| ANOVA |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  |  | Sum of Squares | df | Mean Square | F | Sig. |
| lightness | Between Groups | 986.241 | 9 | 109.582 | 3.073 | .001 |
|  | Within Groups | 35300.544 | 990 | 35.657 |  |  |
|  | Total | 36286.785 | 999 |  |  |  |
| redness | Between Groups | 94.627 | 9 | 10.514 | 4.968 | .000 |
|  | Within Groups | 2095.264 | 990 | 2.116 |  |  |
|  | Total | 2189.891 | 999 |  |  |  |
| yellowness | Between Groups | 588.756 | 9 | 65.417 | 8.146 | .000 |
|  | Within Groups | 7950.724 | 990 | 8.031 |  |  |
|  | Total | 8539.480 | 999 |  |  |  |

Table A10: Analysis of the total variance of the mean L*, a*, and b* colors on silk fibers after testing for lightfastness using short-wave UV irradiation, comparing the influence of different flower extracts

| ANOVA |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  |  | Sum of Squares | df | Mean Square | F | Sig. |
| lightness | Between Groups | 2250.884 | 9 | 250.098 | 4.219 | .000 |
|  | Within Groups | 58687.114 | 990 | 59.280 |  |  |
|  | Total | 60937.998 | 999 |  |  |  |
| Redness | Between Groups | 129.016 | 9 | 14.335 | 7.623 | .000 |
|  | Within Groups | 1861.633 | 990 | 1.880 |  |  |
|  | Total | 1990.649 | 999 |  |  |  |
| yellowness | Between Groups | 1209.541 | 9 | 134.393 | 18.050 | .000 |
|  | Within Groups | 7371.088 | 990 | 7.446 |  |  |
|  | Total | 8580.629 | 999 |  |  |  |

Table A11: Analysis of the total variance of the mean L*, a*, and b* color values ​​on cotton fibers after passing the lightfastness test with short-wave UV irradiation to compare the influence of different mordants

| ANOVA |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  | Sum of Squares | df | Mean Square | F | Sig. |
| lightness | Between Groups | (Combined) |  | 32216.526 | 19 | 1695.607 | 408.253 | .000 |
|  |  | Linear Term | Contrast | 426.088 | 1 | 426.088 | 102.590 | .000 |
|  |  |  | Deviation | 31790.438 | 18 | 1766.135 | 425.234 | .000 |
|  | Within Groups |  |  | 4070.259 | 980 | 4.153 |  |  |
|  | Total |  |  | 36286.785 | 999 |  |  |  |
| redness | Between Groups | (Combined) |  | 1783.101 | 19 | 93.847 | 226.088 | .000 |
|  |  | Linear Term | Contrast | 185.607 | 1 | 185.607 | 447.147 | .000 |
|  |  |  | Deviation | 1597.494 | 18 | 88.750 | 213.807 | .000 |
|  | Within Groups |  |  | 406.790 | 980 | .415 |  |  |
|  | Total |  |  | 2189.891 | 999 |  |  |  |
| yellowness | Between Groups | (Combined) |  | 6158.527 | 19 | 324.133 | 133.413 | .000 |
|  |  | Linear Term | Contrast | 6.907 | 1 | 6.907 | 2.843 | .092 |
|  |  |  | Deviation | 6151.621 | 18 | 341.757 | 140.667 | .000 |
|  | Within Groups |  |  | 2380.952 | 980 | 2.430 |  |  |
|  | Total |  |  | 8539.480 | 999 |  |  |  |

Table A12: Analysis of the total variance of the mean L*, a*, and b* color values ​​on silk fibers after passing the lightfastness test with short-wave UV irradiation to compare the influence of different mordants

| ANOVA |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  | Sum of Squares | df | Mean Square | F | Sig. |
| lightness | Between Groups | (Combined) |  | 56253.133 | 19 | 2960.691 | 619.330 | .000 |
|  |  | Linear Term | Contrast | 3637.609 | 1 | 3637.609 | 760.931 | .000 |
|  |  |  | Deviation | 52615.524 | 18 | 2923.085 | 611.463 | .000 |
|  | Within Groups |  |  | 4684.865 | 980 | 4.780 |  |  |
|  | Total |  |  | 60937.998 | 999 |  |  |  |
| redness | Between Groups | (Combined) |  | 1351.223 | 19 | 71.117 | 108.996 | .000 |
|  |  | Linear Term | Contrast | 237.032 | 1 | 237.032 | 363.280 | .000 |
|  |  |  | Deviation | 1114.191 | 18 | 61.900 | 94.869 | .000 |
|  | Within Groups |  |  | 639.426 | 980 | .652 |  |  |
|  | Total |  |  | 1990.649 | 999 |  |  |  |
| yellowness | Between Groups | (Combined) |  | 4877.164 | 19 | 256.693 | 67.925 | .000 |
|  |  | Linear Term | Contrast | 61.797 | 1 | 61.797 | 16.352 | .000 |
|  |  |  | Deviation | 4815.367 | 18 | 267.520 | 70.790 | .000 |
|  | Within Groups |  |  | 3703.466 | 980 | 3.779 |  |  |
|  | Total |  |  | 8580.629 | 999 |  |  |  |